Combining high efficiency with good radiation tolerance, perovskite solar cells (PSCs) are promising candidates to upend expanding space photovoltaic (PV) technologies. Successful employment in a Near-Earth space environment, however, requires high resistance against atomic oxygen (AtOx). This work unravels AtOx-induced degradation mechanisms of PSCs with and without phenethylammonium iodide (PEAI) based 2D-passivation and investigates the applicability of ultrathin silicon oxide (SiO) encapsulation as AtOx barrier. AtOx exposure for 2 h degraded the average power conversion efficiency (PCE) of devices without barrier encapsulation by 40% and 43% (w/o and with 2D-PEAI-passivation) of their initial PCE. In contrast, devices with a SiO-barrier retained over 97% of initial PCE. To understand why 2D-PEAI passivated devices degrade faster than less efficient non-passivated devices, various opto-electrical and structural characterications are conducted. Together, these allowed to decouple different damage mechanisms. Notably, pseudo-J–V curves reveal unchanged high implied fill factors (pFF) of 86.4% and 86.2% in non-passivated and passivated devices, suggesting that degradation of the perovskite absorber itself is not dominating. Instead, inefficient charge extraction and mobile ions, due to a swiftly degrading PEAI interlayer are the primary causes of AtOx-induced device performance degradation in passivated devices, whereas a large ionic FF loss limits non-passivated devices.

https://doi.org/10.1002/smll.202311097